| Purolite® A600 |  |
| --- | --- |
| Gel Type 1 Strong Base Anion Exchange Resin 强碱性苯乙烯系阴离子交换树脂 BASIC FEATURES:Application - Efficient Demineralization / Silica Removal - Mixed Beds混床阴树脂. Polymer Structure - Gel polystyrene crosslinked with divinylbenzene. Appearance - Spherical beads混床. Functional Group - Type 1 Quaternary Ammonium. Ionic Form as Shipped - Cl- 出厂形式：氯型. Total Capacity (min.) 体积交换容量; 1.4 eq/l (30.6 Kg/ft3) (Cl- form). Moisture Retention, Cl- Form 含水量; 43 - 48 %. Particle Size Range 粒度; 300 - 1200 µm. <300 µm (max.)最小粒度%; 1 %. Uniformity Coefficient (max.); 1.7. Reversible Swelling, Cl- → OH- (max.)转型率; 20 %. Specific Gravity湿真密度; 1.09. Shipping Weight (approx.) 装载密度; 685 - 720 g/l (42.8 - 45 lb/ft3). Temp Limit, Cl- Form氯型耐温; 100°C (212°F). Temp Limit, OH- Form 耐温; 60°C (140°F).. |